## Slide 1
RESEARCH PROPOSAL PRESENTATION
Development of Nano-Reinforced
Bio-Based Adhesives for
Particleboard Manufacture
Presented by
Rashedul Sardar
Student ID: MS-260509
Forestry and Wood Technology Discipline
Khulna University

## Slide 2
Introduction
02
Why develop improved adhesives for particleboard?
Nano-based adhesives offer a promising approach to improving the bonding performance of wood-based composites through nanoscale reinforcement.
Conventional UF-based systems are effective, but formaldehyde emissions and moisture sensitivity remain concerns.
Bio-based tannin can support renewable-resource use, while nano-silica may enhance adhesive performance.
This study will incorporate nano-silica into a tannin–UF adhesive system to evaluate its effects on particleboard properties and identify the optimum concentration.
BIO-BASED
Tannin from Acacia catechu bark
NANO-REINFORCED
Nano-silica as the main variable
TARGET
Strong, moisture-resistant particleboard
FORESTRY AND WOOD TECHNOLOGY | KHULNA UNIVERSITY

## Slide 3
Research Objectives
03
01
Develop
Develop a nano-reinforced bio-based adhesive for particleboard manufacture.
02
Optimize
Optimize nano-silica concentration while maintaining the base adhesive components.
03
Evaluate
Evaluate physical, mechanical, moisture-related and thermal performance.
04
Identify
Identify the formulation that provides the best overall particleboard performance.
FORESTRY AND WOOD TECHNOLOGY | KHULNA UNIVERSITY

## Slide 4
Methodology
04
1
Materials
Tannin, UF resin, nano-silica and hexamine; mango wood chips (1–3 mm).
2
Formulation
Keep tannin and UF fixed; vary nano-silica from 0 to 2.5%.
3
Dispersion
Stir at 600 rpm for 15 min, then ultrasonicate for 10 min.
4
Board manufacture
Dry chips to 2–4% moisture; apply 10% adhesive; hot-press at 170°C, 10 MPa, 10 min.
5
Testing & analysis
Test density, moisture content, water uptake, thickness swelling, linear expansion, MOR, MOE and IB; analyze with SPSS.
FORESTRY AND WOOD TECHNOLOGY | KHULNA UNIVERSITY
SEM image of nano silica particles.

## Slide 5
Expected Outcomes, Timeline & Conclusion
05
Expected Outcomes
Improved strength, moisture resistance, thermal stability and durability.
Greater use of renewable biomass and reduced dependence on conventional adhesive systems.
Potential contribution to SDGs 9, 12 and 13.
Research Activities & Timeline
Jul–Aug 2026
Literature review
Aug–Oct 2026
Material collection & characterization
Oct–Dec 2026
Formulation & optimization
Dec 2026–Jan 2027
Particleboard manufacture
Jan–Mar 2027
Performance & durability tests
Mar–May 2027
Analysis, writing & submission
Conclusion
The study will identify an effective nano-silica-reinforced tannin–UF adhesive formulation and evaluate its suitability for stronger, more durable particleboard.
FORESTRY AND WOOD TECHNOLOGY | KHULNA UNIVERSITY

## Slide 6
References
06
Bardak, T., Sozen, E., Kayahan, K., & Bardak, S. (2018). The impact of nanoparticles and moisture content on bonding strength of urea formaldehyde resin adhesive. Drvna industrija, 69(3), 247–252. https://doi.org/10.5552/drind.2018.1755
Cui, Z., Xu, Y., Sun, G., Peng, L., Li, J., Luo, J., & Gao, Q. (2023). Improving bond performance and reducing cross-linker dosage of soy protein adhesive via hyper-branched and organic–inorganic hybrid structures. Nanomaterials, 13(1), 203. https://doi.org/10.3390/nano13010203
Roumeli, E., Papadopoulou, E., Pavlidou, E., Vourlias, G., Bikiaris, D., Paraskevopoulos, K. M., & Chrissafis, K. (2012). Synthesis, characterization and thermal analysis of urea–formaldehyde/nanoSiO₂ resins. Thermochimica Acta, 527, 33–39. https://doi.org/10.1016/j.tca.2011.10.007
Zhu, Z., Zhang, E., Zeng, Q., Rao, J., & Chen, N. (2022). Graphene oxide functionalized cottonseed-lignin resin with enhanced wet adhesion for woody composites application. Polymers, 14(1), 1. https://doi.org/10.3390/polym14010001
FORESTRY AND WOOD TECHNOLOGY | KHULNA UNIVERSITY

## Slide 7
THANK YOU
Questions & Discussion
Rashedul Sardar | MS-260509
Forestry and Wood Technology Discipline, Khulna University